REPORT OF ANALYSIS

The sample was submitted by client with the following identification :

| CLIENT | : | SCG LIGHTWEIGHT CONCRETE INDONESIA, PT. |
| --- | --- | --- |
| ADDRESS | : | Jl. Surya Tekno Kav. I – T1 – 3. Surya Cipta City of Industry, Kutamekar, Ciampel. KARAWANG – JAWA BARAT 41361. |
| TYPE OF SAMPLE | : | GYPSUM. |
| DATE RECEIVED | : | 13/08/2018. |
| TEST REQUIRED | : | Chemical Analysis. |
| DESCRIPTION OF SAMPLE | : | Form : Soil. Weight/Volume : ± 1.18 kg. Packing : Plastic bag. |
| SAMPLE IDENTIFICATION | : | Code: Gypsum Clariant. |
| DATE OF ANALYSIS | : | 13/08/2018 to 23/08/2018. |
| YOUR REFERENCE | : | -- |

- Result:

| Parameter | Unit | ##### Results | Method |
| --- | --- | --- | --- |

| Iron Trioxide (Fe2O3) | % | 3.36 | ASTM C 471-2014 |
| --- | --- | --- | --- |
| Aluminium Trioxide (Al2O3) | % | 7.11 | ASTM C 471-2014 |
| Magnesium Oxide (MgO) | % | 0.68 | ASTM C 471-2014 |
| Manganese Dioxide (MnO2) | % | 0.11 | ASTM C 471-2014 |
| Chromium Trioxide (Cr2O3) | % | Less than 0.01 | ASTM C 471-2014 |
| Sodium Oxide (Na2O) | % | 0.13 | ASTM C 471-2014 |
| Potassium Oxide (K2O) | % | 0.06 | ASTM C 471-2014 |
| Silicon Dioxide (SiO2) | % | 3.19 | ASTM C 471-2014 |
| Titanium Dioxide (TiO2) | % | 0.02 | ASTM C 471-2014 |
| Phosphorus Pentaoxide (P2O5) | % | 0.03 | ASTM C 471-2014 |
| CaSO4.2H2O based on SO3 | % | 41.50 | ASTM C 471-2014 |
| Insoluble Residue | % | 1.63 | ASTM C 471-2014 |
| Calcium Carbonate (CaCO3) | % | 17.54 | ASTM C 471-2014 |
| Calcium Oxide (CaO) | % | 23.33 | ASTM C 471-2014 |
| Sulfur Trioxide (SO3) | % | 19.30 | ASTM C 471-2014 |
| Combine Water | % | 26.00 | ASTM C 471-2014 |
| Free Moisture 45oC | % | 15.65 | ASTM C 471-2014 |

Note  :  AR (As Received Basis).

This Certificate/report is issued under our General Terms and Conditions, copy of which is available upon request or may be accessed at www.sucofindo.co.id

|  | SBU Mineral |
| --- | --- |
| CBT5001296185010 | Dedih Budiawan Sugianto |